[image: ]        用于GMF锌镍铁合金钝化工艺
Trivalent Chromium Iridescent Passivator  SS-152 三价铬五彩钝化剂      技术资料
                      
Trivalent Chromium Black Zinc Passivator TCP-976
三价铬黑锌钝化剂（碱性镀锌钝化剂)
一、Features
1. TCP-976 trivalent chromium black passivator contains no hexavalent chromium, silver or other harmful metals, fully complying with environmental protection regulations.
2. This product is exclusively applied to alkaline zinc plating and produces a dark, uniform black passivation film.
3. It is a two-component passivating solution. Combined with PB-952 sealant after black passivation, the salt spray resistance of the coating can be greatly enhanced. The coating can withstand more than 96 hours of salt spray test without white corrosion spots.

2． [bookmark: _GoBack]Operating Parameters

	Item
	Optimum Value
	Operating Range

	TCP-976A
	Barrel plating: 120 ml/LRack plating: 90 ml/L
	80–150 ml/L50–100 ml/L

	TCP-976B
	Barrel plating: 50 ml/LRack plating: 90 ml/L
	40–60 ml/L60–120 ml/L

	Temperature
	30 °C
	20–40 °C

	pH Value
	2.2
	1.8–2.5

	Processing Time
	Barrel plating: 30 s ; Rack plating: 60 s
	30–60 s

	Agitation
	Continuous tank circulation
	—

	Filtration
	Recommended
	—



3． Bath Make-up

1.Fill the tank with half the required volume of water.
2.Add the required amount of TCP-976A and stir thoroughly.
3.Add the required amount of TCP-976B and stir evenly.
4.Top up the solution to the standard working volume.
5.Test and adjust the pH to the recommended range using nitric acid and sodium hydroxide solution while stirring continuously. Adjust the solution temperature to the specified range.

东莞市硕美电子材料科技有限公司                                       Page  1 / 3
TEL：0769-81030039，     FAX：0769-81030059，       热线：13925851538 裴先生
地址：广东省东莞市桥头镇田头角村银岭街63号D栋一楼  E-mail:peter@dgsomei.com  官网: www.dgsomei.com 
东莞市硕美电子材料科技有限公司                                     Page   2 / 3
TEL：0769-81030039，    FAX：0769-81030059，      热线：13925851538 裴先生
地址：广东省东莞市桥头镇田头角村银岭街63号D栋一楼  E-mail:peter@dgsomei.com  官网: www.dgsomei.com
image1.png
SOMEI 30 £ 4t 2




